Grade: re-NY66-1200

Molding Grade PA 66 with 50% Pre-consumer Validated Recycled Content Materials

**Typical Material Properties**

|  |  |  |  |
| --- | --- | --- | --- |
| **Physical** | **Nominal Values** | **ASTM Test** |  |
| Specific Gravity | 1.14 | D792 |  |
|  |  |  |  |
| **Mechanical** |  |  |  |
| Tensile Strength @ Yield  Flexural Modulus | 11,200 psi  400,000 psi | D638  D790 |  |
|  |  |  |  |
| **Impact** |  |  |  |
| Notched Izod Impact (73 °F, 0.125 in) | 0.8 ft-lb/in | D256 |  |
|  |  |  |  |
| **Thermal** |  |  |  |
| Melting Temperature | 496 °F | D3418 |  |
|  |  |  |  |
|  |  |  |  |

The information provided above is based upon typical values and are intended only as guides. Star Plastics, LLC, assumes no obligation or liability for any advice furnished or for any results obtained with respect to this information. *No guarantees or warranties are expressed or implied.*

\*reNova® is a registered trademark of Star Plastics, LLC, its subsidiaries or affiliates.

**Recommended Processing Guidelines**

|  |  |  |
| --- | --- | --- |
|  | **Nominal Values** |  |
| Drying Time and Temperature | 2-6 hrs at 176-212°F |  |
| Suggested Max Moisture | <0.20% |  |
| Rear Temperature | 482 – 536 °F |  |
| Middle Temperature | 527 – 554 °F |  |
| Front Temperature | 527 – 554 °F |  |
| Nozzle Temperature | 527 – 563 °F |  |
| Processing (Melt) Temperature | 500 – 580 °F |  |
| Mold Temperature | 150 – 220 °F |  |
|  |  |  |
|  |  |  |

The conditions listed above are only guidelines. You may want to adjust conditions to meet your requirements.